## Slide 1: AlGaAs Electro-optic (initial) measurement
Danny Vander-Hyde , Stefan Ballmer, and Steve Penn
LVK update
September 2020
Notes: AlGaAs = crystalline coating, introduces a Pockels effect
Looking to get a calibrated displacement measurement from this Electro-optic effect for AlGaAs coatings to see its potential contributions to the LIGO noise budget

## Slide 2: Normal E-field injection (basic construction)
Figure elements do not
reflect realistic scaling
Notes: Electrode plates:
  Aperture diameter : 3 mm
  Plates diameter : 76.2 mm
  Plate separation : 9 mm
  Voltage across electrodes : 300 V
Optic:
  Optic diameter : 25.4 mm
  Optic thickness : 7 mm
  Material : Fused silica
    Amorphous coating mirror
      SiO2 /Ta2O5
    AlGaAs mirror

## Slide 3: 3D printed enclosure / optic mount
Notes: Brigham young university compliant mechanisms research orthoplanar spring design

## Slide 4: Experiment schematic
Vout(f)
Notes: Did not explicitly measure A2 but the calibration factor shows very deviation beyond unity across all measured frequencies hence we assume a DC value of A2 based on the laser spec sheets will suffice until A2 is explicitly measured with a cavity sweep
Input mirror T = 578.5 ppm
Amorphous coating end mirror T = 593.2 ppm
AlGaAs mirror T = 39.9 ppm
Difference in Finesse between the two cavities:
Amorphous coating end mirror cav : 5.37e3
AlGaAs mirror cav : 10.2e3

## Slide 5: Single frequency measurement
Notes: Still need to measure open loop gain for algaas mirror cavity

## Slide 6: Single frequency measurement
Notes: One model point (field inside coating)

## Slide 7: Where does this model estimate come from?
Calculating (reflection phase) for coating
Numerical Poisson computation used to estimate field strength normal to surface of optic (Ez)

## Slide 8: estimate for HR AlGaAs coating
= 4.5 x 10-10 [rad]/[V/m]
x = 3.8 x 10-17 [m/V/m]
Notes: Electro-optic effect estimate
Treatment analogous to thermo-optic effect
Temperature coefficient  electro-optic coefficient
Assume incident light is polarized along the [110] crystallographic direction
2 pi / half fringe (or 2pi of phase shift in reflection per half wavelength)

## Slide 9: Numerical Poisson calculator results (potential map)

## Slide 10: Numerical Poisson calculator results
Slightly inside optic media
( behind front face
and inside coating)
Notes: Change wording here so it is just outside and inside

## Slide 11: Next measurements
Harmonics measurement
Frequency sweep measurement from 300 Hz to 5 kHz
Measure dn/dE + dL/dE effects for controlled non-normal fields
  Alternative split electrode design
Notes: 300 when signal disappears in noise
Suspected laser pzt resonances

## Slide 12: Thank you!

## Slide 13: References
Fejer, M.M. , Electro-optic Effects in AlGaAs mirrors , (2018)
Cahillane, C., Initial Electric Field Meter Results For Advanced LIGO and Beyond, (2018)
BYU CMR, Ortho-planar spring design : https://www.thingiverse.com/thing:3007261

## Slide 14: Extra Slides

## Slide 15: Electro-optic effect estimate
Treatment analogous to thermo-optic effect
  Temperature coefficient  electro-optic coefficient
Assume incident light is polarized along the [110] crystallographic direction
and are the high and low index layers respectively
is the electro-optic coefficient for GaAs (and is assumed the same here for AlGaAs)

## Slide 16: What the DAQ sees
And we can say so :
M, and (f)
is laser PZT gain, currently from spec sheet, will measure with cavity sweep

## Slide 19
RC lowpass pole at 146 Hz due to HVA resistance
Artifact at 5 kHz due to HVA bypass crossover
Notes: RC low pass 100 Hz due to HVA amplifier resistance
@ 5kHz there is a switch off to the passive components
(SUGWG elog 412) https://sugwg-alog.phy.syr.edu/aLOG/index.php?callRep=412

## Slide 21
Pole @ 60 kHz
= 1/
C = 1/ = 1 / = 2.65e-10 F

## Slide 22: LHO X-end Electric Field meter noise ASD
Say ambient field [V/m
And assuming and order of magnitude estimate (based on model and measurement) of [m/V/m]
Strain:
  A+ : 7.82*10-23
Credit : Craig Cahillane