## Slide 1: Experiment to measure the Pockels effect from an HR AlGaAs coating (update)
Danny Vander-Hyde , Stefan Ballmer, and Steve Penn
LVK March 2021

## Slide 2: Pockels Effect (quick summary)
Same physics used in electro-optic modulators (dn/dE)
For AlGaAs HR coating (grown along [001] crystallographic direction):
Where (-1.2e-12 [m/V]) is the electro-optic coefficient and and coating respectively
A
= 3.8*10-17 [m/V/m]

## Slide 3: Experiment layout
Notes: PDH locked cavity with modulated voltage to electrodes from 1kHz to 30kHz

## Slide 4: Electric field estimate within coating
E-field estimate at ROI:
6350 [V/m]

## Slide 5: Measurable using in-air cavity

## Slide 6: 3D printed optical mount
Ortho-planar spring design for pitch and yaw control

## Slide 7: Previously reported single frequency drive results

## Slide 8: Frequency sweep test (SiO2-Ta2O5 sample mirror)

## Slide 9: Next Steps
Further investigation as to why we see the drive coupling into the PDH error signal for SiO2/Ta2O5 sample
  Potential mechanical instability of 3D printed mount
  Electronics crosstalk
Once aforementioned coupling is addressed, attempt to measure Pockels effect with AlGaAs sample
Investment in calibration sample
Measure effect with separate individual polarizations

## Slide 10: Refrences
Fejer, M.M. , Electro-optic Effects in AlGaAs mirrors , (2018)
Yariv, A., 1988, Quantum electronics, 3rd edn, (John Wiley & Sons)
BYU CMR, Ortho-planar spring design : https://www.thingiverse.com/thing:3007261

## Slide 11: Thank you!
Questions? Suggestions?

## Slide 12: EXTRA SLIDES

## Slide 13: Frequency sweep test (both sample mirrors)

## Slide 14: Calibration
This frequency response measurement records the following ratio in dB of the following:
We also know that the error signal spectra of the loop is probed by :
Where is the uncalibrated voltage output from the mixer, is the FSS transfer function, and is the open loop gain of the PDH system.

## Slide 15: Calibration (cont.)
And we know so :
Where are a high voltage amplifier response and measured response of the laser piezo respectively. is the sample cavity length, is the laser frequency.
Substitute (1) into (4):
M,
and ,

## Slide 17: OLG

## Slide 18
A(f)

## Slide 19: Voltage on front electrode plate (swept frequency measurement)

## Slide 20
FSR
MHz / V
Notes: Laser PZT response
Between first TEM00 and HG01 mode 1946923 Hz / V
Between first TEM00 and second TEM00 mode 2009867 Hz / V